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	Technical data sheet
	Date: 03.05.2009

	
	Supplier
	Customer: Producta srl

	Compound: EPDM 60
	Self Life: 21 days
	Colour: Black
	Application: Building Profiles

	Standard : DIN 7863 B - UNI 9122 – ISO 815
	Type of Application: Extrusion LCM/UHF
	Working Temperature: 

- 35 ÷ + 100°C
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	RAW COMPOUND CHARACTERISTICS

	Properties
	Method
	U.M.
	Specification
	Obtained Value

	Mooney Viscosity ML(1+4) 100° C
	ISO 289
	M.U.
	67 ÷ 82
	71,5

	Mooney Scorch t5@ 121 °C
	ISO 667
	min.
	
	

	Rheometer

■ MDR ± 0,5° 3 min 185° C
□ ODR ± 3°    min    °C
(*) dNm for MDR - lb x in for ODR
	ASTM D 6204

ASTM D 2084


	
	MDR
	ODR
	

	
	
	(*)
	ML= 2,4 ÷ 3,1
	
	2,75

	
	
	(*)
	MH= 12,0 ÷ 15,0
	
	13,40

	
	
	min
	Ts2= 0,52 ÷ 0,65
	
	0,59

	
	
	min
	T30 = 0,59 ÷ 0,74
	
	0,66

	
	
	min
	T60= 0,82 ÷ 1,02
	
	0,92

	
	
	min
	T90= 1,60 ÷ 2,00
	
	1,81


CHARACTERISTICS OF THE COMPOUND VULCANIZED AT THE FOLLOWING CONDITIONS:
	■ PLATELETS thickness 2 mm 

Vulcanized at 164 °C for 20 minutes
	■ DISK thickness 6 mm

Vulcanized at 164 °C for 30 minutes

	Properties
	Method
	U.M.
	Specification
	Obtained Value

	Specific gravity
	ISO 2781
	g/cm3
	1,16 ÷ 1,20
	1,175

	Hardness
	DIN 53505
	ShA
	66 ( 4 (**)
	67,0

	Tensile strength (TS)
	ASTM D 412
	Mpa
	>9,0
	9,9

	Elongation at break (EB)
	ASTM D 412
	%
	≥ 200
	375

	Ozone resistance 96h, 20% elong., 40°C, 50pphm O3
	UNI 6067
	
	No crack
	No crack

	
	
	
	
	

	Properties after air-oven ageing for 70 h at 100 °C
	Din 53508
	
	
	

	Δ Hardness
	DIN 53505
	Points
	+ 10 max
	+ 5

	Δ Tensile Strength
	ASTM D 412
	%
	- 20 max
	+ 2,5

	Δ Elongation at Break
	ASTM D 412
	%
	- 35 max
	- 28,6

	Δ Weight
	UNI 8313
	     %
	± 3
	- 0,3

	Properties after air-oven ageing for 168 h at 100 °C
	DIN 53508
	
	
	

	Δ Hardness
	DIN 53505
	Points
	-5 ÷ +15
	+ 6

	Δ Tensile Strength
	ASTM D 412
	%
	- 25 max
	+ 6,7

	Δ Elongation at Break
	ASTM D 412
	%
	- 50 max
	- 29,5

	Compression Set 22h at 25°C def. 25%
	DIN 53517
	%
	
	8,0

	Compression Set 22h at 100°C def. 25%
	DIN 53517
	%
	≤ 35
	26,5

	Compression Set 70h at 100°C def. 25%
	DIN 53517
	%
	≤ 35
	33,7

	Compression Set 22h at - 25°C def. 25%
	DIN 53517
	   %
	≤ 70
	68,3

	Properties after low temperature for 168 h at - 10 °C
	DIN 53508
	
	
	

	Δ Hardness
	DIN 53505
	Points
	+ 10 max
	+ 4

	NOTE (**)

The value is measured on the laboratory specimen obtained by molding. On the final extruded product, depending on continuous curing conditions, the hardness should be 60 ± 5, according to the standard DIN 7863 B.

The storage time is guaranteed only with the respect of the conditions in the document CDS 004 and in the point 7 of the Material Safety Data Sheet.

The information and data referred to “OBTAINED VALUE” are believed to be accurate and are given in good faith but they aren’t contractual parameters.

However, accuracy is not guaranteed and no warranty to obtain the same results in other laboratory.

Confirmation and/or updating of the found values and relative tolerances could be defined after bigger production volumes.
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